深圳市驰普电子科技有限公司

CHEAPE TECHNOLOGY INTERNATIONAL LTD

Acknowledgment

| Customer Name | Chi Pu electronic | Productmodel | XR453048 |
| --- | --- | --- | --- |
| Delivery date | 2012-10-25 | Configuration | 5460(208)+8205*2+10K |
| Revision |  | Page | 03 | Revision | A1 |
| Approved | TO examine | Elaboration |
| Material Number |  |
| Customer confirmation column |
| Confirm comments： Signature： Date： |
| Special Note: Customer receive samples promptly after test,the test results will be back to my company FAX:0755-61186524, to facilitate the company to arrange for the project follow-up work, 5 days without any reply,the company for customers to test qualified default,the project ended normally. Customer test qualified,please indicate the product customer feedback column names and product code,and stamped signature confirmation,otherwise please test unqualified column indicate te problem,put forward the improvement proposal. My company received after customer signed original and enclose the product description functional description,in order to receive orders. |

# Contents

1 Outline

This specification is suitable 2-serial-cell Lithium ion Battery Protection circuit manufactured by ctechi TE CO.,LTD

2 Application

- Lithium-ion rechargeable battery packs

- Lithium-ion polymer battery packs

3 Electrical characteristics

| Item | Content | Criterion |
| --- | --- | --- |
| Over charge Protection | Monomer overcharge protection voltage | 4.25±0.025V |
|  | Monomer overcharge release voltage | 4.05±0.05V |
| Charge protection | Rated charging current | ≤2A |
|  | Charge current protection | / |
| Over discharge protection | Single discharge protection voltage | 2.40±0.06V |
|  | Monomer overdischarge release voltage | 3.0±0.075V |
|  | Nominal discharge current | ≤3A |
|  | Discharge current protection | 10±3A |
| Short protection | There is no short-circuit protection | Yes |
|  | Protection of short circuit current | / |
|  | Short circuit protection restoration condition | Disconnect the load |
| Temperature protection | Thermal protection temperature | / |
|  | Recovery temperature/time | / |
| Balanced | Balanced voltage | / |
|  | Equilibrium current | / |
| Interior resistance | P+,P-conduction resistance | ≤40mΩ |  |
| Current consumption | Self power consumption | ≤15μA |  |
| (L*W*H) Size | 29*7.2*1.0mm Tolerance：±0.1MM |  |

4 Wiring diagram

Prot description：

1、B+：Connect the battery cells positive

2、B-：Connect the battery core negative

3、P+：Connecting the output charge / discharge anode

4、P-：Connecting the output charge / discharge cathode

5、B2-/B1+：Connecting the two batteries are connected in series between the

6、T：Test port